## Slide 1: R150 RRD Retro-reflective Devices
Simplification stage 2
SLR-39-01/Rev.2
(Rev. of SLR-38-08/Rev.2)

## Slide 2: Resistance to weathering
Annex 13 and 22
Weathering with xenon-arc weathering device
Evaluation by reference materials blue wool – grey scale
State of the art test, defined parameter in refrenced ISO 4892-2
Annex X (new)
Weathering with xenon-arc weathering device
Defined time of 500 h
Evaluation by set up minimum level for specific coefficient of retroreflection at 80% of required values
Evaluation of colour as defined in R48
Justification

## Slide 3: Resistance to weathering
Methode applicable for retroreflective sheeting material used for
  retroreflective markings of
  Classes C, D, E, F
  Classes 1, 2, 3, 4, 5
  and SMV Class 1 and 2
Not applicable for retroreflectors of
  Classes IA, IB, IIIA, IIIB and IVA
  Advance Warning Triangle of Type 1 and 2

## Slide 4: Annex 24 Examples of Approval Marks
Adjustment of the sizes of the approval marks
  In Table 1, to reduce the number of minimum sizes of “a”, the value “4 mm” should become “5 mm” and the value “12 mm” should become “8 mm”.
Changes in the examples of the approval marks
  Space removed for class IIIA
  Sice alligned
  „104R“ removed
  „27R“ replaced by WT

## Slide 5
Retro-reflective devices | Symbol | Minimum “a” for examples of figures in Annex 24 (values in mm) | Paragraph
Retro-reflector for motor vehicles (independent) | IA | 5 | 5.1.
Rear retro-reflector for motor vehicles (combined with other signal lamps which are not watertight) | IB | 5 | 5.1.
Retro-reflector for trailers (independent) | IIIA | 5 | 5.1.
Rear retro-reflector for trailers (combined with other signal lamps which are not watertight) | IIIB | 5 | 5.1.
Rear wide-angle retro reflector | IVA | 5 | 5.1.
Conspicuity marking (material for contour/strip marking) | C | 8 | 5.2.
Conspicuity marking (material for distinctive markings/graphics intended for a limited area) | D | 8 | 5.2.
Conspicuity marking (material for distinctive markings/graphics intended for an extended area) | E | 8 | 5.2.
Conspicuity marking (materials for distinctive markings or graphics as base or background in printing process for fully coloured logos and markings of class "E" in use which fulfil the requirements of class "D" materials) | D/E | 8 | 5.2.
Retro-reflective materials for extremities marking of class F | F | 8 | 5.2.
Retro-reflective marking for long or heavy vehicles (retro-reflective and fluorescent materials) Marking plate of class 1 or class 2 | RF | 5 | 5.2.
Retro-reflective marking for long or heavy vehicles (retro-reflective only materials) - Marking plate of class 3, class 4 or class 5 | RR | 5 | 5.2.
Marking for slow moving vehicles (retro-reflective and fluorescent materials) - Marking plate of class 1 | RF | 5 | 5.2.
Marking for slow moving vehicles (retro-reflective only materials) - Marking plate of class 2 | RR | 5 | 5.2.
Advance Warning Triangle (Type 1) | T1 | 8 | 5.3
Advance Warning Triangle (Type 2) | T2 | 8 | 5.3
Table 1
List of retro-reflective devices and their symbols

## Slide 6
See new pages 7 and 8
Space removed
E
4
3333
IA
2b
R2
F2
AR
S2
148R00
150R01
Size aligned
104R replaced by 150R
27R replaced by WT
E
4
IIIA
150R01 216
a/3
a/3
a/2
a/3
a
E
4
C
150R01 1148
a/3
a/2
a/3
a
E
4
WT
150R01 4216
a/3
a/3
a/2
a
a/3
a/3

## Slide 7
Space removed
104R replaced by 150R
27R replaced by WT
E4
IIIA
150R01 216
a
a/2
a/3
a/3
a/3
E1
C
150R01
1148
E3
WT
150R01
4216
Make sure to add sentence like in Annex 7 of 148 or Annex 13 of R149

## Slide 8
Figure YYY - Marking example ZZ
Existing examples in R148 Annex 7 and R150 (real size of the marking)
E4
IA 2b R2
148R00
3333
150R00
F2 AR S2
E4
IA 2b R2
148R00
3333
150R00
F2 AR S2
E
4
3333
IA
2b
R2
F2
AR
S2
148R00
150R01
Size aligned