## Slide 1: An Outlook on Thermal Runaway Initiation & Propagation Testing
UN GTR No. 20 – EVS22
October 2021

## Slide 2: GTR No. 20 Background
Phase 1
Documentation Requirements for Manufacturers
Phase 2
Thermal Runaway (TR) Propagation Test is under consideration
The methods of thermal runaway initiation under consideration are:
(1) Rapid Heating Method
(2) Nail Penetration Method

## Slide 3: Thermal Runaway Propagation Test Methods
New: GTR 20 Phase 1 Test Procedure
Drill Hole position and direction are selected
Hole is drilled in the enclosure of the battery system
Nail is inserted
Nail perforates the cell causing TR
Localized Rapid External Heating Method
Nail Penetration Test
New: ISO 6469-1:2019/CD AMD1 (Section 6.7.7)
Thermal Runaway Initiation Method (TRIM)
  Developed by National Research Counsel (NRC) Canada2
A high-powered heat pulse is applied to a small area on the cell’s external surface until TR is achieved
2 Source: “Localized Rapid Heating Methodology and Testing Fully Operational Vehicles” Presented by Transport Canada to NHTSA, February 23, 2021.
A
B

## Slide 4: Thermal Runaway Test Methods - Possible Challenges
Possibly Intrusive & potentially compromises the battery pack
May not be representative of the heat output, gas emissions, and ignition characteristics
Cell Selection for TR Initiation - Difficult
TR Initiation Methods may not be representative of actual fault conditions and lack objectivity
Perforation Depth of Nail & Direction may vary
Nail penetration may damage more layers
  Result: higher heat output than in an actual fault condition
Rechargeable Electrical Energy Storage System (REESS) Modification for Surface Mounting:
  Risk potentially altering REESS functionality
May result in heating more than one cell
If heater is inserted between 2 cells, risk TR initiation in 2 cells simultaneously
Heater Selection (power & size) dependent on cell size & type
Nail Penetration Test
Rapid Heating Method
General
A
B
Unclear if these Test Methods Achieve: Feasibility, Objectivity (Repeatability & Reproducibility), Practicability across all EV Makes & Models

## Slide 5: Research Objectives
Evaluate
Feasibility, Objectivity, and Practicability of test methods on different REESSs
Compare
Test results from the heating method with results from the nail penetration method

## Slide 6: Test Matrix
Vehicle Model | Rapid Heater Test | Nail Penetration Test
A | 2 | 0
B | 1 | 1
C | 1 | 1
D | 1 | 1
I.
III.
I.
4 Vehicle Models with different battery cell technology (e.g. cylindrical, prismatic, etc.)
II.
Repeated on 1 Vehicle Model twice to evaluate repeatability
Conducted on 3 (new) EVs
IV.
Comparison of heating method & nail penetration test results for the same (but new) vehicle models
IV.
III.
II.