## Slide 1: Li-Ion Battery Pack Immersion Exploratory Investigation
UN GTR No. 20 – EVS 22
October 2021

## Slide 2: Li-Ion Battery Pack Immersion Exploratory Investigation
Immersion of an electrified vehicle’s battery pack is a relatively infrequent occurrence in the real world
Seven batteries were tested for immersion as well as post-immersion smoking or fire.
Report published August 2021
Previous testing published in 2019

## Slide 3: Existing Immersion Standards
SAE J2464 NOV2009 – 4.3.5 Immersion Test (Module or Pack Level)
  “With the DUT in its normal operating orientation and at full state of charge, immerse the DUT in ambient temperature salt water (5% by weight NaCl in H2O) for a minimum of 2 hours or until any visible reactions have stopped ….” (SAE International, n.d.)
USABC Battery Abuse Testing – 4.4 Water Immersion
  “Salt water should be an approximation of seawater (3.5% (600 mM, 35 ppt) sodium chloride)…. The DUT should remain immersed for (1) a minimum of 2 hours or (2) until failure of the DUT (HSL ≥5).… DUT should be monitored for at least 30 minutes after the completion of the test.” (Orendorff et al., 2017)
ISO 6469-1:2019 – 6.4.2 Immersion into Water
  “Immerse the DUT in ambient temperature salt water (3.5-5% by weight) for 2 hours” + 2 hours post-immersion observation time. Requirements: No fire, no explosion.” (International Organization for Standardization, 2019)

## Slide 4: Test Program
Test Asset # | Battery Type | Capacity | Key Test Parameters
1 | PHEV | 8.8 kW-hr | Frequent immersion and observation intervals every 15 minutes
2 | BEV | 16 kW-hr | 30-minute immersion time and 1 hour observation time
3 | BEV | 30.5 kW-hr | Immersion and observation intervals every 15 minutes for 45 minutes.
4 | BEV | 32.9 kW-hr | 2-hour immersion and 2-hour observation
5 | BEV | 60 kW-hr | 1-hour immersion time + 2-hour observation
6 | BEV | 60 kW-hr | 1-hour immersion time + 2-hour observation. 0.1 percent Salinity
7 | PHEV | 8.9 kW-hr | Short duration initial immersion of 20 minutes prior to first observation period. 0.1 percent Salinity
Batteries were immersed near 100% capacity or the expected maximum charge
level achieved during normal vehicle charging.
Samples were selected from a range of manufacturers
5 batteries immersed with 3.5% salinity; 2 tests used reduced salinity to resemble coolant fluid

## Slide 5: Test Setup

## Slide 6: Battery Immersion

## Slide 7: Immediately After Immersion & 10 minutes later

## Slide 8: Observations
All the batteries degraded with no adverse reaction while immersed
2 batteries had smoke/venting issues post-immersion:
  1st Battery was immersed for 20 minutes in water (3.5% salinity)
  2nd Battery was immersed for 15 minutes in water (0.1% salinity)
Primary reactions during immersion appeared to last between roughly 30 minutes and 1 hour. Larger capacity batteries took longer.
Post immersion batteries were under 50V
Battery degradation/discharge occurred quicker in 3.5% salinity water.
Based off the research completed to date, a battery immersion test in water of lower salinity (<0.1% NaCl) and shorter immersion duration (<30 min) would be more stringent than a test with longer immersion duration (2 hours) in sea water (3.5% salinity).