## Slide 1: TP-TF report for 26th IWG meeting
2023.4
EVS-GTR

## Slide 2: Outline
01 Recent work & meeting
02 Round-table discussion
03 Next-step work

## Slide 3: 01 Recent work & meeting
Nov-Dec, 2023——25th IWG meeting
  TP-TF report
  Technical report
  Draft proposed by EU/JRC
Feb, 2023 ——TP-TF meeting
  Round table discussion for key topics: Initiation method, criteria of thermal runaway and vehicle/component level test.
Mar, 2023——Solicit feedback of draft
Apr, 2023——Pre-observation and updated draft

## Slide 4: 02 Round-table discussion——A. Initiation method
Background
In the current regulation draft, localized rapid external heating from ISO 6469-1 AMD1:2022 is the only mentioned initiation method.
Question
Do you think alternative methods are necessary?
If alternative method is necessary, What’s the relationship of these methods?
  Equivalent options
  Main method and alternative method

## Slide 5: 02 Round-table discussion——A. Initiation method
Discussion summary
Alternative initiation method is necessary: CN、JP
  Technology neutrality and feasibility considering different design and technologies
  The validity of alternative initiation method is judged by whether TR is successfully initiated.
Alternative initiation method is not necessary: EU, CA, KR
  Equivalency of main alternative methods should be confirmed.
Mixed opinions: OICA
Temporary no feedback: US

## Slide 6: 02 Round-table discussion—— B. Criteria of thermal runaway
Background
In the current regulation draft, the criteria of thermal runaway is as follows:
Main criteria
Thermal runaway can be detected by the following conditions:
(i) The measured voltage of the initiation cell drops, and the drop value exceeds 25% of the initial voltage;
(ii) The measured temperature of the initiation cell exceeds the maximum operating temperature defined by the manufacturer;
(iii) dT/dt ≥ 1 °C/s of the measured temperature of the initiation cell for at least 3s.
Supplementary criteria
The following indicators can be considered as supportive evidence of occurrence for thermal runaway:
— dP/dt ≥ 0.01 bar/s of the measured pressure in the pack for at least 3s;
— smoke release;
— occurrence of ejected solid material;
— failure of the BMS or signal faults (if the BMS is still active). Logged faults in the BMS shall be analysed. Thermal runaway indicators shall be specified and documented if required.
The following indicators are post-analysis criteria as evidence of whether a thermal runaway has occurred in the initiation cell and whether this has resulted in thermal propagation in the REESS or REESS subsystem:
— mass loss greater than its electrolyte mass of the initiation cell;
— REESS or cell rupture;
— REESS deformation;
— material formation indicating high temperatures (e.g. molten and re-solidified aluminium or copper);
— specific reaction products such as e.g. metallic nickel or cobalt, lithium-aluminium oxide;
— current collector foil absence (partial or total);
— thermal decomposition of polymer materials, e.g. separator, isolation material.
Thermal runaway can be judged when:
(a) Both (i) and (iii) are detected;
(b) Both (ii) and (iii) are detected; or
(c) At least two supplementary criteria and (iii) are detected.

## Slide 7: 02 Round-table discussion—— B. Criteria of thermal runaway
Post-analysis is not suitable for homologation purpose
ISO 6469-1 AMD: 2022 should be considered as a reference
Some parameters were suggested to be added into criteria of thermal runaway
  Pressure
  Temperature of heater
Discussion summary

## Slide 8: 02 Round-table discussion——C. Test level
Background
In the current regulation draft, only vehicle level test is proposed
Discussion summary
Component level is necessary: CN, JP, KR, OICA
  Low cost and easy to implement
  Vehicle level TP test is challenging for heavy-duty vehicle
Component level isn’t necessary: EU, US, CA
  TP could occur faster in the vehicle level other than component level in the test showed by JRC
  Equivalency between component and vehicle level should be confirmed

## Slide 9: 03 Next-step work
Considering limited time and large number of comments for the draft, the effective way to proceed the TP test should be discussed.
Next TP-TF meeting will be held between 26th and 27th IWG meeting (meeting date is still need to be discussed between TF-leaders).

## Slide 10: Thanks