## Slide 1: Tyres and abrasion Ice and 3PMSF tyres Action item TA-12-03
TA-14-06

## Slide 2: ICE and 3PMSF tyres on IFV circuit, dry roads
At “low” temperature (5°C, more normal use of ice tyre) abrasion rate of ice tyre is equivalent to abrasion rate of 3PMSF tyres
At "high" temperature (16°C), not recommended for ice tyre, the abrasion rate of the ice tyres is significantly higher than 3PMSF tyres.
Chart: Test IFV circuit, 1 ice tyre, 3 3PMSF @ 4°C and 16°C
| 3PMSF 1 | 3PMSF 2 | 3PMSF 3 | ICE 1
4C | 34.0606 | 50.1904 | 50.1267 | 57.028
16C | 39.7019 | 66.3188 | 66.026 | 98.4667

## Slide 3: ICE and 3PMSF tyres on Finland circuit, icy roads (-11°C) & dry roads (16°C)
Under ice and snow conditions (-11°C; ca. 90% “non-Asphalt” conditions) Abrasion Rate is for all tyres significantly low.
Under elevated temperatures (5°C; 99% bare Asphalt conditions, 42% wet) Abrasion Rate is for all tyres is higher. In this example 3PMSF tyre shows the highest Abrasion Rate.
Chart: Test Finland, 3 ice tyres, 1 3PMSF tyres @ -11°C and 5 °C
| 3PMSF | ICE 1 | ICE 2 | ICE 3
-11C | 18.0503 | 11.9497 | 11.0692 | 12.2642
5C | 125.5975 | 81.0063 | 107.4843 | 81.9497

## Slide 4: Many thanks for your attention

## Slide 5: Ice Grip Tyres facts summary
Ice Grip Tyres is a subcategory of 3PMSF tyres, they fulfill the Ice Grip Test limit described in R117
Ice Grip Tyres were originally developed as an environmentally friendly alternative to studded tyres
Ice grip tires are designed for icy and snowy road conditions
  Abrasion is minimal on icy and snowy road conditions
  Ice grip tires have different temperature behavior compared to other winter tires
  Testing locations and time period for suitable testing conditions (low temperature, dry asphalt without snow and ice) would be very limited or not existing
  To be representative, need to run ~80% on icy road (very variable condition impossible to control), with ~ no abrasion, with relevant X and Y accelerations
  New extremely strict temperature range requested, with high operational difficulties to run the test in the representative conditions (when very cold weather, often snow on road, test has to stop)
  New reference tyres could be needed
Seasonal tire change is done in Nordic countries in spring and autumn
  In Sweden over 93,2% of motorists change from winter tires to summer tires for the summer months
  In Nordic countries the average maximum temperature in winter is ≤ 3°C
The market volume of ice grip tires (Nordic non-studded winter tires) is low both in Europe and globally
  4.1% of winter tires in Europe, 1.2% of all tires in Europe and used only in Nordic countries