|  | United Nations |  |  |
| --- | --- | --- | --- |
|  | Economic and Social Council |  |  |

Economic Commission for Europe

Inland Transport Committee

World Forum for Harmonization of Vehicle Regulations

Working Party on Pollution and Energy

Proposal for a new UN GTR on In-vehicle Battery Durability for Electrified Heavy Duty Vehicles

Submitted by the Informal Working Group on Electric Vehicles and the Environment (EVE)*

UN Global Technical Regulation on In-vehicle Battery Durability for Electrified Heavy Duty Vehicles

Contents

…..

…..

[Editorial Note: This technical rationale has used the GTR22 equivalent as a starting point – updating and modifying accordingly]

I.	Statement of technical rationale and justification

A.	Introduction

1.	Owing to the pressing need to reduce emissions of greenhouse gases (GHG) and other air pollutants, the market share of electrified vehicles is expected to grow in the future. A key component of these vehicles is the traction battery that is used to store and deliver energy to power the movement of the vehicle and the systems within it. Improvements in the performance of batteries to deliver increased driving range, reduced charging times and greater affordability are a significant focus for manufacturers and technological developments in this area are expected to accelerate the uptake of electrified vehicles by consumers.

2.	Electrification is also extending to heavy-duty vehicles, such as buses, coaches and trucks above 3,855 kg, albeit at a much lower speed given their size, weight and specificities. One key difference with light-duty vehicles is that for several truck categories, a significant share of the energy stored in the vehicle is used for purposes other than propulsion. For example, for cooling in the case of refrigerated trucks for the transport of food or certain medical supplies; concrete mixers, where most of the energy is used to mix concrete. The primary motivation for this GTR therefore stems from the recognition that the environmental performance of electrified heavy-duty vehicles may be affected by excess degradation of the battery system over time. It builds on the adoption of the United Nations General Technical Regulation No. 22 providing minimum performance requirements for the battery durability of electrified light-duty vehicles by the World Forum in March 2022 and its amendment in June 2024.

3. This GTR applies to vehicles of categories 1–2 and 2, that have a technically permissible maximum laden mass equal or exceeding 3,855 kg, that (a) are HD-PEV or HD-OVC-HEV vehicles, and (b) have an originally installed batteries as defined in this GTR. At the option of the Contracting Party, a lower minimum technically permissible maximum laden mass may be used.

4.  The Contracting Party shall make a decision about the applicability of this GTR to Small Volume Manufacturers and special purpose vehicles and special axle formulas for their jurisdiction

5. Vehicle category trailers and semitrailers, which may be electrified in future, are excluded from this version of the GTR.

6.	Loss of vehicle energy efficiency and loss of electric range are both primary concerns. Loss of electric range could lead to a loss of utility, meaning electric vehicles are driven less and therefore displace less distance travelled that might otherwise be driven in conventional vehicles. Loss of vehicle efficiency could impact the upstream emissions by increasing the amount of electricity needed per vehicle distance travelled. Both can affect not only the utility of the vehicle to the consumer, but also the environmental performance of the vehicle. Loss of environmental performance is important, in particular because governmental regulatory compliance programs often credit electrified vehicles with a certain level of expected environmental benefit, which might not be realized over the life of the vehicle if excess battery degradation occurs.

7.	In addition to changes in range and energy consumption, hybrid electric vehicles are often equipped with both a conventional and electric powertrain, and for these vehicles the criteria pollutant emissions from the conventional powertrain could be impacted by the degradation of the battery over time.

8.	This GTR therefore aims to provide a harmonised methodology to address these concerns by introducing a method by which the health of the battery can be monitored over time and introducing minimum performance requirements for the durability of the battery in an optional annex. In order to address regional considerations, a Contracting Party may optionally elect to enforce Minimum Performance Requirements (MPRi) from these tables.

B.	Procedural background

6.	The Informal Working Group (IWG) on Electric Vehicle and the Environment (EVE) was set up in June 2012 following the approval by WP.29/AC.3 of ECE/TRANS/WP.29/AC.3/32. This document established two distinct IWGs to examine environmental and safety issues related to Electric Vehicles (EVs): the IWG on EVE, reporting to the Working Party on Pollution and Energy (GRPE), and the IWG on Electric Vehicle Safety (EVS), reporting to the Working Party on Passive Safety (GRSP). The proposal was supported by the European Commission, the United States of America, China, and Japan.

7.	A second mandate for the IWG on EVE, divided into Parts A and B was approved in November 2014 by AC.3 to conduct additional research to address several recommendations that grew out of the first mandate, and develop UN GTR(s), if appropriate. The second mandate was separate from the IWG on EVS.

8.	Part A of the second mandate of the IWG on EVE (ECE/TRANS/WP.29/AC.3/40) included “battery performance and durability” as one of the topics authorized for study and potential GTR development. Specifically, Part A authorized activity “to further develop the recommendations for future work outlined in the Electric Vehicle Regulatory Reference Guide by: (i) conducting additional research to support the recommendations; (ii) identifying which recommendations are suitable for the development of (a) global technical regulation(s) (GTR(s)) by the World Forum for Harmonization of Vehicle Regulations (WP.29); and (iii) developing a work plan. The work of the IWG on EVE on battery performance and durability under Part A of the EVE mandate was reported to WP.29 in a status report as informal document WP.29-170-31 at the 170th meeting of WP.29, 15-18 November 2016.

9.	At the close of Part A the IWG on EVE recommended that GRPE and WP.29 endorse the option of extending the mandate of the IWG on EVE to continue active research into the topic of battery performance and durability without committing to the development of a GTR at that time. This was endorsed and work continued on this topic within Part B of the mandate.

10.	The IWG on EVE presented a draft status report to GRPE in May 2019 on the research on in-vehicle battery durability and performance. The status report indicated that there was sufficient information to allow a UN GTR for in-vehicle battery durability to be started. The IWG on EVE recommended at the 79th GRPE in May 2019 that the UN GTR on in-vehicle battery durability be developed under a new mandate.

11. The EVE IWG published UN GTR No.22 (In-Vehicle Battery Durability for Electrified Vehicles), in the UN Global Registry on March 09, 2023.

12. Due to the focus of UN GTR No. 22 on light-duty vehicles and developments in the heavy-duty vehicle sector, the EVE IWG has been authorized to begin development of a new standalone UN GTR on in-vehicle battery durability for electrified heavy-duty vehicles, at the 190th session of World Forum for Harmonization of Vehicle Regulations (WP.29), which will be developed in 2 phases:

Phase 1:

(a)	Initial draft development and working document submission to GRPE and AC.3 for consideration as a new UN GTR

(b)	Consider alternative test methods including chassis dynamometer testing.

Phase 2:

(a)	Continue development of alternative test methods including chassis dynamometer testing.

(b)	Future amendments as new data and continued research, analysis and testing lead to new developments.

C.	Technical background

Battery degradation in electrified vehicles

13.	The effect of battery degradation on environmental performance is likely to differ significantly among the various electrified vehicle architectures (Pure Electric Vehicle (PEV), Off-Vehicle Charging Hybrid Electric Vehicle (OVC-HEV) and Not Off-Vehicle Charging Hybrid Electric Vehicle (NOVC-HEV)). The primary forms of battery degradation are capacity degradation and power degradation. Capacity degradation is the loss of energy capacity, resulting in a loss of electric driving range (for PEVs and OVC-HEVs) and possibly increased use of the engine during hybrid operation (for NOVC-HEVs). Power degradation is the loss of battery power, which can also lead to increased use of the engine for OVC-HEV and NOVC-HEVs and possibly reduced performance of the vehicle overall.

14.	There are at least six major vehicle operating parameters that affect in-vehicle battery durability. Each differs in importance depending on electrified vehicle architecture:

(a)	Discharge rates, as determined by vehicle duty cycle and operator use including, but not limited to, vehicle speed, auxiliary loads, towing, payload and ambient conditions;

(b)	Charge rates, as determined by type (normal, ultra-fast, Mega Watt Charging System (MCS), dynamic charging systems) and frequency of charging;

(c)	State of charge (SOC) window used in system operation of the battery and the amount typically used between charge events (depth of discharge);

(d)	Battery temperature during operation (operation includes all temperature exposures from vehicle purchase through retirement, both while being operated and during periods of charging and inactivity);

(e)	Time (calendar life);

(f)	Other uses not reflected in calendar life or distance travelled, such as Vehicle to (V2X), that is, Vehicle to Grid, to Facility, to Home, to Load, or any Power Take-Off (PTO)/auxiliary operations or not-traction purposes during stand-still but also in motion.

15.	The extent and nature of battery degradation that will occur is a result of complex mechanisms and heavily dependent on the battery cell chemistry and operating conditions. A variety of physical and electrochemical processes influence the durability of battery cells and these have been documented comprehensively within a literature review commissioned by the IWG on EVE. For typical lithium-ion batteries the primary mechanisms leading to capacity degradation were summarised as:

(a)	Loss or deposition of cyclable lithium or a loss of balance between electrodes;

(b)	Loss of electrode area; and

(c)	Loss of electrode material or conductivity.

16.	These aging processes are often further complicated by the fact that many of the mechanisms are associated with a rise in cell impedance, leading to a reduction in maximum cell power.

Management of battery degradation

17.	Whilst manufacturers have found it possible to establish the durability of specific battery implementations sufficiently to bring the products to market with some degree of confidence that normal provisions for customer satisfaction and warranty terms are being met, not every manufacturer is establishing durability in the same way. Manufacturers employ a wide variety of testing regimes often tailored to specific product configurations, applications, customer groups, and geographic considerations.

18.	To reduce the effect of capacity degradation, manufacturers may choose to slightly oversize a PEV or OVC-HEV battery to allow the battery performance to be maintained by widening of the state-of-charge (SOC) window to make more energy capacity available as capacity degrades. Others may choose to account for degradation by warranting the battery to a specified degree of capacity retention over a specified period of time or distance travelled. In the latter case, the consumer is expected to understand that a potential reduction in the usable battery energy is to be expected during the life of the vehicle.

19.	A number of further measures are employed by manufacturers to limit battery degradation. These typically include, but are not limited to, the use of properly optimised battery management systems (BMS) and battery thermal management. BMS can reduce stress on the battery and prolong battery life by controlling some operations to protect the battery cells, maintain cell charge balancing and moderate the battery temperature. For example, BMS might control enhanced cooling systems, limit fast charging events through modulation of the charging current, control the available state of charge window, keep the cell voltages balanced, or reduce the maximum available torque as necessary to protect battery health. The inputs to BMS can include anything from ambient conditions and driver behaviour to individual cell metrics. Each manufacturer, vehicle, battery and cell could have unique and highly optimised BMS, that are updated and improved with every iteration. BMS are very complex and generally considered highly proprietary and should not be tampered with out of environmental and safety concerns. Another important factor is the battery thermal management capability. While some batteries are only passively cooled by ambient air, others are actively cooled and heated by use of forced air, liquid coolant, or refrigerant, which leads to greater BMS control over battery operating temperature and hence longer life.

Prediction and/or estimation of battery degradation

20.	Accelerated aging is a familiar technique used by many manufacturers as a component of their battery durability testing methods. This technique assumes that a regime of rapid aging cycles can be translated to a projected useful life in service. However, it is uncertain whether the translation from accelerated aging to an in-use life projection is equally applicable to all forms of lithium-ion chemistries either currently in use or in the future.

21.	One of the major mechanisms by which capacity and power degradation occurs in these chemistries is the microscopic fragmentation that accompanies swelling and contraction of anode and cathode materials during cycling. Specific chemistries differ significantly in this respect, suggesting that the relation between rapid cycling and long-term cycling may also differ significantly. An accelerated test that accurately projects useful life for one chemistry may therefore predict poor life for another chemistry, even though both chemistries may achieve an equal life in actual use.

22.	Furthermore, accelerated ageing cannot take into account the real use of batteries inside vehicles and therefore can only partially estimate the real degradation.

23.	To monitor degradation in-use, most manufacturers employ some form of in situ, on-board capacity estimation through the BMS. This estimation can vary in accuracy and precision depending on a number of factors including the sensors and estimation algorithm used, the charge/discharge behaviour of the user, and the cell type and cell model parameters. Proprietary algorithms are used to handle inaccuracies and output an estimate that can be utilised by other systems within the vehicle.

24.	There are currently no requirements on the accuracy of on-board monitors and the estimates generated are not typically easily accessible to the vehicle user. The IWG on EVE has therefore made a decision to set the performance requirement in this field.

D.	Technical rationale and justification

25.	The mandate of the first phase of this GTR on in-vehicle battery durability includes the development of an initial draft development and working document based on the equivalent GTR for light duty vehicles (GTR No. 22), modified accordingly to take account of the different context, issues and requirements associated with heavy-duty vehicles. It will be based on the development of: (a)	Requirements for reading and/or displaying battery health information and usage data from the vehicle;

(b)	Requirements for electrified vehicle battery durability performance criteria; and

(c)	A provisional in-service conformity test which will include generic usage criteria and a statistical method.

(d)	A reference certification procedure to check compliance against

26.	This section sets out the key considerations of the IWG on EVE in developing the respective elements of Phase 1 of the GTR as set out above.

State-of Certified Energy (SOCE) monitors

27.	Whilst the term State of Health (SOH) is commonly applied to refer to the health of a battery at a given point in its life, this term is not commonly defined and is determined through a variety of different methodologies. It was therefore chosen to define  a new related metric for use within the GTR: the State of Certified Energy (SOCE). This metric represent a percentage of the certified battery energy remaining at a given point in time. In the case of SOCE, it was decided to base the metric on the Usable Battery Energy (UBE).

28.	A metric based upon UBE was chosen and is based on key performance parameters relating to battery health. This metric is intended to provide both the basis of information made available to consumers and also values for assessment against Minimum Performance Requirements (MPR) relating to battery durability by manufacturers and authorities if elected to be enforced by regional authorities. The IWG decided to exclude NOVC-HEVs from the GTR development. While batteries of NOVC-HEVs can experience degradation, NOVC-HEVs have no electric range, and their battery UBE is not typically determined at certification. Moreover, battery degradation in an NOVC-HEV is likely to result in degradation of fuel economy, which can be detected by existing in-service conformity practices. [The IWG will continue to consider the need for extending this GTR to NOVC-HEVs in the future].

30.	From discussions within the IWG while developing the GTR No. 22 it was concluded that it would not be appropriate to define the process or algorithm by which the SOCE monitors determine their estimated values. It would be highly complex to define an algorithm that could accurately account for the battery management strategies in use within the market. Instead, it was determined to allow manufacturers to determine their own means to estimate these metrics, whilst ensuring the accuracy through an in-use verification procedure. This was also considered true for heavy-duty vehicles.

Battery performance requirements

31.	The key battery durability requirements set out within this GTR are defined in terms of MPR. MPR are expressed as a minimum allowable value of SOCE after a given length of time, distance travelled or energy utilised. This follows a similar format applied by manufacturers when providing warranty for electrified vehicles.

31.	In determining appropriate MPR values for this GTR the IWG on EVE considered inputs from stakeholders within the IWG, which is summarised paragraphs 32. to 37. below.

32.	Warranty analysis was conducted by the UK to understand the current warranty offering from manufacturers for electric heavy duty vehicle batteries. The review primarily focussed on the UK market, but values were also consistent with typical offerings within other market. The review showed that batteries are covered for failure for .

33.	The European Commission’s Joint Research Centre (JRC) has developed a dedicated in-vehicle battery durability assessment module within its ‘Transport tEchnology and Mobility Assessment’ (TEMA) platform. This is based on performance-based models as this class of models is the most suitable to be used with large-scale real-world driving data. TEMA is a modular big data platform designed to reproduce mobility behaviours of vehicles from datasets of navigation system data of conventional fuel vehicles and quantify possible impacts of new vehicle technologies on real-world mobility while supporting transport policy assessment.

34.	TEMA combines recent performance-based capacity and power fade models for Lithium-ion batteries from literature with information on battery and vehicle architectures, together with real world vehicle driving data from different geographical areas of Europe, to develop a scenario-based analysis for predicting in-vehicle performance degradation of automotive traction batteries. The analysis includes the calendar and cycle capacity fade of different Lithium-ion variants (LiFePO4, NCM with spinel Mn, NCM-LMO, NCA, NCM-LTO, LFP-LTO,…) in different vehicle architectures (OVC-HEV and PEV of different driving range segments for LDVs and vehicle categories for HDVs), combined with different recharging strategies reflecting use-cases for passenger and commercial vehicles to explore the effect of different driving duty cycles related to different mobility patterns and mission profiles and environmental temperatures.

35.	The TEMA model was extended to address e-HDVs battery ageing estimating the energy capacity retention of traction batteries after a range of distances, time periods and energy throughput the battery to allow consideration of appropriate choices for MPR for the different HDV categories and mission profiles. The TEMA model explored e-HDVs in-vehicle battery durability scenario studies based on both the 2019/1242/EU regulation vehicle categories, mission profiles and annual mileages and data of vehicles from literature reviews obtaining similar results with the two methods. New recharging strategies resembling the most common recharges foreseen for HDVs (ultra-fast, MCS, opportunistic or at deposit,…) have been integrated within TEMA together with PTO applications, such as, concrete mixer, crane, construction or garbage pressing from literature.  A good correlation was found between the results of the simulations and the warranties data overview provided in the EVE-61-08e presentation. The simulation results suggested  the possibility  to group different vehicle categories and mission profiles for suggesting common MPRs.

36. Example TEMA modelling results in Figure I/1 for HD-PEV of category 2 vehicles not exceeding 16 tonnes and mission profiles either charged with ultra-fast charging or MCS at lunch time show greater than 75  per cent capacity retention after 8 years or 300,000 km and xx MWh of energy throughput and 70 per cent capacity retention after 10 years or 375,000 km,  while for category 2 vehicles exceeding 16 tonnes and mission profiles either charged with ultra-fast charging or MCS at lunch time  show greater than  60  per cent capacity retention after 12 years or 700,000km and xx MWh of energy throughput and 55  per cent capacity retention after 15 years or 875,000km. This result is generally consistent with prevailing warranty practice observed in the warranty survey. It has to be noted that the results referred to worst case scenario of battery ageing, extrapolating the validity of the model, to suggest not so stringent MPRs in view of future revision of the battery performances based on data from the field. An additional 5 per cent of margin has been added to the values as first proposal.

Figure I/1

Example of a capacity retention curve generated from JRC TEMA modelling for different HD-PEV categories and mission profiles

37. The TEMA model has also been exercised to reproduce some data from literature referring to in-services buses in China with good comparison of the predictions despite the different assumptions to mimic the buses mission profiles. Overall, the published study incorporates 240 million rows of raw data from 60 electric vehicles operating for over 4 years. 38. MPR values were also proposed by Japan and CATARC. Japan proposed the same value of 70 per cent capacity retention after 6 years or 150,000km for all the vehicle categories (Category 2 and 1-2), while CATARC differentiated the MPR for vehicle category and mission profile, based on China field data.

39. ….

40.	Following consideration of the available evidence and views of stakeholders within the IWG on EVE, a set  of MPR values were introduced in an optional Annex based upon different time and distance combinations with an eventual future correlation to the energy throughput metric, set in monitoring in the first phase. This approach allows coverage of the wide range of different distance-based or PTO applications requirements needed across Contracting Parties and provides the option for a Contracting Party to optionally apply MPR and metric as appropriate for their market. Attention was given to a possible correlation between  the different vehicle classes and groups around the regions for the MPR and metric of the tables of the optional Annex 4 of the GTR. Following discussion within the IWG, the same MPR were set for OVC-HEVs and PEVs.

41.	Electrified vehicles of categories 1–2 and 2, that have a technically permissible maximum laden mass equal or exceeding 3,855 kg are at an earlier stage of adoption within the fleets of many Contracting Parties and subsequently in-use data relating to battery durability is scarce for these vehicles. For this reason, the collection and monitoring of from field- data is recognised to be of key importance for the future revision of the MPRs and metric.  It was highlighted by manufacturers that the understanding and estimation of PTO currently presents an increased challenge compared to only drive and charge behaviour. A concept related to virtual distance was introduced to cover the V2X, PTO and non-traction purpose of the vehicles similar to GTR No. 22 but adapted for HDVs.

42.	Battery longevity is a key consideration for consumers and regulating agencies, therefore there is an incentive for manufacturers to accredit batteries that perform beyond the minimum requirements of this GTR. To allow manufacturers to market or quantify the benefits of any improved battery technology they may have installed within their vehicles the GTR also allows for a Declared Performance Requirement (DPR) to be proposed by manufacturers, based upon a higher value of SOCE. To ensure the accuracy of any declared values, the DPR would be considered to act in place of the MPR for the purposes of in-use verification. The DPR is not intended to indicate a regulatory warrantied value. Manufacturer warranties are beyond the scope of this GTR. A manufacturer may wish to warranty batteries beyond the MPR without attaching additional warranty benefits to a DPR.

In-use verification

43.	To ensure the accuracy of the SOCE monitors and also ensure that MPR are being met a two part in-use verification process has been introduced as in the GTR No. 22, with Part A verifying the accuracy of the monitors and Part B verifying the battery durability against MPR, where applicable. The Part C verification of the accuracy of the virtual distance was included in this GTR  to address HDV PTO, V2X and non-traction purpose.

44.	Part A verification verifies the accuracy of the SOCE monitor in the vehicles by comparing the read and measured SOCE value for a sample of vehicles. It involves the measurement of the UBE under the defined test procedures of the Annex 3 of the GTR  and determination of a measured SOCE by dividing the UBE measured value by the respective values from certification [derived with the same test procedure, if applicable]. [The same test method must be applied at certification to the SOCE monitor family  concerned  and during in-service testing Part A  verification, if applicable and in accordance to regional  provisions, unless there is an agreement between the regional authority and the manufacturer.]

45. These measured values can then be compared to the on-board values from the SOCE monitors to ensure the accuracy is within a specified tolerance. A pass or fail decision on a sample of vehicles will be reached through a statistical process, which evaluates the average of the differences of the  measured and on-board-indicated SOCE from a series of vehicles tested. After testing a minimum of 3 vehicles a decision on either a pass or fail decision or on testing a further vehicle will be reached, on the basis of a statistical formula considering the quantitative deviation of the latter average from a value A and the variance of these differences over the whole test series with a tolerance = 5% granted for a single test due to technical reasons. The method proposed is particularly suitable for cases where a quantity (such as SOCE) is likely to differ from the ‘true’ measured quantity continuously and reflects the method used for evaluating the conformity of production (CoP) in UN Regulation No. 154 and in the GTR No. 22.

46. The resolution of the on-board values from SOCE was set to 1 part in 100, and the required accuracy defined by a statistical process as described above.

478. In the case of HDV, there is not a reference certification test procedure at vehicle level to be referred to for the measurement of the UBE. Therefore, the EVE IWG aimed at defining a test procedure allowing the UBE determination by testing the battery in the vehicle. Moreover, the test procedure shall allow a repeatable and robust UBE measurement, but without being excessively and unduly demanding, given the size and variety of heavy duty electrified vehicles on the market and relative scarcity of suitable testing facilities worldwide.

48. The European Commission Joint Research Centre (JRC) presented a proposal to measure the UBE using a bi-directional power supply in a temperature-controlled environment, ensuring proper preconditioning of both the vehicle and the battery and controlling the discharge power to be representative of the vehicle use. The measurement of the UBE by a discharge at constant power using a bi-directional power supply has been considered as a suitable compromise between the feasibility of the test and its accuracy.

49.In order to ensure the feasibility of the test for all Contracting Parties and for all types of heavy duty electrified vehicles, even those that do not allow battery discharging through a power supply, it was proposed and then agreed to adopt three types of tests for the measurement of the UBE, plus an alternative method based on a chassis dynamometer:

- Method 1a: Discharge by driving on a test track using characteristic regional speeds

- Method 1b: Discharge by driving on the road using average speed

- Method 2: Discharge using a bidirectional power supply system

- Alternative method: discharge  using constant and transient cycles test method by using a HDV chassis dynamometer

50. A technical breakout group was set up lead by the European Commission Joint Research Centre (JRC) to discuss and define the boundary conditions  of the test procedures. In particular, the topics of acceleration to the target speeds of Method 1a and Method 1b, the average speed setting and discharge power tolerances, the end-of-discharge conditions, the driver breaks, and all the other influencing factors of the test procedures, such as, road gradients and the ambient temperature,  were discussed and a proposal was prepared for the whole EVE IWG. The  test repetitions for enhancing the test results  were also addressed together with the charging power settings. During the EVE IWG meeting 69th it was considered appropriated to remove the test repetitions for all the test methods, due to the extra test burden caused by applying test repetitions.

51. Method 1a and Method 1b  have a less controlled temperature. A provision has been added to guarantee the consistency of the UBE measured results at type approval and in-service testing by requiring a soak and pre-conditioning at given temperature and allowing the operation of internal pre-warming system of the battery, if available. External pre-warming systems, different from charging stations, are not allowed. For taking into account of the road grading in Method 1b  the proportional cumulative positive altitude gain over the entire trip was added requiring that it shall be less than 1,200m / 100km.

52. The test ends with a fully discharged battery when the break-off criterion is reached, specifically defined for the different test methods and vehicle configurations.

53. A specific discussion was around the break-off criterion for the different test methods for both HD-PEVs and HD-OVC-HEVs. A 4 consecutive second or more driving power cut criterion was introduced for HD-PEVs tests while for HD-OVC-HEVs a new criterion related to the variation of the energy consumption in the last defined km driven during the test in respect to the energy consumption over the total driven distance minus the last defined km. For the alternative method criteria similar to LDVs dyno tests were introduced as options to be elected by the Contracting Party.

54. [It is allowed to use static battery discharging systems in the last part of the test to complete the discharge if agreed with the responsible authority during Method 1b, to comply to the safety rules in place. The discharge power of the system should be representative of the characteristic driving speed. The break off is reached when the discharging power experience a drop of [5kW] for 4 seconds. ]

55. In the bi-directional power supply system method the discharge takes place at a constant power derived from the characteristic speed of the vehicle, in a temperature-controlled environment. The test ends with a fully discharged battery when the [prescribed discharge power cannot be maintained for more than four seconds].

56. The chassis dynamometer testing was retained as an alternative method. This method, which is more similar to the test procedure for LDVs, was initially discarded for HDVs, due to the limited availability of testing facilities worldwide, and the complexity of the test procedure. Constant and transient cycles test methods using HD chassis dynamometer refer to regional regulations.

57. A test pilot phase was organised by the industry to verify the several steps of the different test procedures and inform the discussion accordingly in support to the drafting of the text of the GTR.

58.	As Part A verification is expected to involve a relatively small number of sample vehicles to limit the testing burden, it is important to ensure that the sample result is not unduly impacted by the abnormal use or poor maintenance of a vehicle within the sample. A vehicle survey has therefore been introduced within Annex 1 containing information designed to ensure that the vehicle has been properly used and maintained according to the specifications of the manufacturer. Any vehicles not meeting the required criteria may be removed from the test sample. Collected from the field data can support future improvement and revision of the Annex 1 requirements.

59.	Due to the accuracy of the SOCE monitor being assured through verification in Part A, it is possible to verify the battery durability of a sample of vehicles within Part B through remote collection of the on-board SOCE value, together with information on the age of the vehicles, distance travelled and energy utilised. Where a vehicle has been equipped with V2X capabilities, PTO applications or non-traction purposes, an equivalent virtual distance will be calculated in relation to the V2X,PTO and non-traction purpose discharge energy. This will be summed with the distance travelled to calculate the total distance. This approach avoids the need for further testing of vehicles within Part B and enables a simple route to the assessment of a large sample size of vehicles, thereby minimising the impact that outliers (e.g. vehicles that have been used abnormally) may have on the sample result.

60.	It is recognised that SOCE values read from a sample of vehicles are likely to be in the form of a distribution, with values for individual vehicles dependent on the vehicle usage and any inherent variation in the performance of the vehicle or traction battery. Where a vehicle has been used abnormally (e.g. with prolonged periods of storage or being regularly used in extremes of temperature) this may also give rise to more significant degradation of battery health. To reduce the impact of vehicles that may have been used abnormally, it was decided to make the overall pass decision dependent on more than or equal to 90 per cent of monitor values read from the vehicle sample being above the MPR. This approach thereby ensures that the MPR is being met by the significant majority of the vehicle sample, whilst accounting for abnormal usage.

61.	To further minimise influence of abnormally used vehicles, a maximum of 5 per cent of the values taken from smaller durability families that consist of less than 500 vehicles may be excluded from the verification sample in Part B with appropriate reasoning. The decision on the number of vehicles in the sample may be taken by the responsible authority based on risk assessment methodology, but in principle should not be less than 500.

62.	To support this two part in-use verification process, whilst minimising the burden of increased testing for manufacturers within Part A, two family concepts were developed within the GTR. This includes the concept of a monitor family for use in Part A and a battery durability family for Part B. This is likely to reduce the need for additional testing where multiple battery durability families may have the same characteristics with respect to verification of the SOCE monitors. In addition, the Part A in-use verification for the vehicles in the same monitor family may be combined between different regions with the agreement of all Contracting Parties involved. This contributes not only to minimise the testing burden but also to increase the verification robustness. However, this concept shall not be applied for Part B since battery deterioration might be different in different regions due to different usage patterns and ambient conditions.

[63. Paragraph 1.1  referring to the vehicle selection during certification and during Part A verification  has been added to clarify to the vehicle testing criteria.]

[64. 	In order to verify that the virtual mileage is reported correctly by the vehicle, an extra verification has been introduced as Part C, together with the definition of a Part C family definition. Different proposals for the verification of  the reported virtual distance have been discussed for the GTR No. 22: with a single test with one to three vehicles, with maximum three vehicles for a fail decision and  with a statistic increasing number of vehicle up to 4 for a pass decision. The EVE IWG reached consensus on this last also for the HDV GTR. An agreed verification procedure use case with an adequate number of vehicles (at least 1 and not more than 4) used in V2X or PTO or not-traction purposes shall be performed. The verification of the reported virtual distance shall lead to a fail in the verification procedure if the reported virtual distance is more than 5% higher than the measured virtual distance.]

65. The family  definition for Part A and Part B, and also Part C  might be subject to review based on field data.

[66. A list of values to be read from the vehicle has been introduced in the Annex 2 of this GTR containing information designed to survey the vehicle usage together with the SOCE. This list of values have been updated in the specific metrics and requirements  to HDVs and other upcoming regulatory frameworks.]

E.	Technical feasibility, anticipated costs and benefits

67.	The use of SOH monitoring within HDV electrified vehicles  and updating these monitors to ensure the specific requirements within this GTR are met and to allow information to be provided to the consumer may entail some development costs for manufacturers.

68.	The Part A verification of SOCE accuracy will involve additional testing by manufacturers and, optionally, by authorities who choose to further verify monitor accuracy.

69.	Any costs associated with verification within Part B are likely to be borne by the authorities of the Contracting Parties applying this regulation and will depend on the extent and means by which they choose to collect data for verification. Costs may be borne by the manufacturer in the case of a fail for a battery durability family relating to the costs of measures agreed with the relevant authorities to bring those vehicles back into compliance.

70.	This GTR is likely to give rise to benefits for manufacturers and authorities through the prevention of inferior products, which could undermine the market. Introduction of inferior products within the market could disadvantage those manufacturers who have invested in the development of technology aimed at ensuring battery longevity and could also undermine the environmental benefits that can arise from electrified vehicles, as well as public acceptance.

71.	The longevity of battery life is a key concern for prospective consumers of electrified vehicles. [The health of a vehicle’s battery upon entry into the second-hand market is also a significant point of consideration for the consumer and is not easily understood in the absence of access to accurate battery health monitors. The availability of both accurate battery health information and assurances on battery longevity for consumers that is provided by this GTR are therefore likely to have a positive impact on the cost retention of electric vehicles and consumer confidence in buying an electrified vehicle].

F.	Future development of the GTR

72.	The mandate for development of this GTR included the future development of improvements to the GTR within Phase 2 that includes, but not limited to:

(a) Continue development of alternative test methods including chassis dynamometer testing.

(b) Future amendments as new data and continued research, analysis and testing lead to new developments.

[73.	The concept of an NUI is a data field stored on the vehicle that represents a history or assessment of lifetime usage patterns of the vehicle that are influential to battery degradation. For example, one NUI might characterise temperature exposures during the life of the vehicle, while another might characterise charging rates or number of fast-charging events. The definition of NUIs was highlighted within the discussions of the IWG on EVE as a technically challenging task that will require further data collection and validation to achieve. It could, however, provide an alternative and more robust means of handling SOCE values recorded from vehicles that have been used abnormally in future. The possibility of incorporating NUIs within this GTR should therefore be explored.]

74.	The implementation of this GTR by Contracting Parties will enable the collection of further data on SOCE to better inform our understanding of battery health degradation. This information will, in turn, allow further refinement of the GTR, including MPR values, based upon the latest available battery technologies employed within the market. This will be important given the rapid development of technology in the field of battery technology for electrified vehicles.

*