## Slide 1
1
Comments on Document WT-02-02
for tyre buffing
Informal document WT-03-03
(3th GRBP WGWT IWG,
Geneva,
10th-11th , September 2019.)
China Automotive Technology and Research Center Co., Ltd.
Notes: 1

## Slide 2: Table of Contents
2
Wear Profile Scenario
Buffing Tolerance
Additional Information
Conclusions

## Slide 3
3
Wear Profile Scenario

## Slide 4: Buffing Machine
4
Driving wheel
Rim base
Grinding wheel

## Slide 5: Buffing Machine Parameters
5
Technical Parameters | 
Tyre outer diameter | PCR/LTR 550mm - 1000mm
Nominal rim diameter | 14'-19'（Depend on test rims, maximum 30'）
Section width of Tyre | PCR/LTR 150mm - 400mm
Control limit of Tyre pressure | Max. 500kPa
Buffing device | Grinding wheel feed speed : 1.2mm/s - 5mm/s
 | Grinding wheel feed speed accuracy : ±0.02mm
 | Buffing tolerance of each measurement point : ±0.2mm

## Slide 6: Tyre Status During The Buffing
6
Before buffing
Before buffing
After 2.45mm offset buffing
After 50% offset buffing
Example 2
Example 1

## Slide 7: Wear Profile Scenario Comments
7
Following the document presented by ETRTO( WT-02-02 ), two scenarios for principal grooves are still under discussion as below:
Comment:
Both scenarios can be achieved according to the current practices.
Additional assessments are needed to determine which scenario is better.
Relevant experiences
Buffing test amounts : Totally 24 Tyres. Buffing tests in 2018:
  Flat profile : 8 tyres.
  Offset profile : 16 tyres.

## Slide 8
8
II. Buffing Tolerance

## Slide 9
9
 | Tyre 1 |  |  |  | Tyre 2 |  |  | 
Groove | B | C | D | E | B | C | D | E
Average tread-depth before buffing | 6.85 | 6.96 | 6.94 | 6.74 | 6.97 | 7.08 | 7.05 | 6.83
Buffing target(2.45mm offset) | 4.40 | 4.51 | 4.49 | 4.29 | 4.52 | 4.63 | 4.60 | 4.38
Average Buffing target | 4.42 |  |  |  | 4.53 |  |  | 
Average Individual tread-depth after buffing | 4.62 | 4.69 | 4.62 | 4.38 | 4.48 | 4.55 | 4.48 | 4.26
Average tread-depth after buffing | 4.58 |  |  |  | 4.45 |  |  | 
Deviation of Average Individual tread-depth | 0.22 | 0.18 | 0.13 | 0.09 | (0.03) | (0.07) | (0.11) | (0.12)
Deviation of Average tread-depth total measurements | 0.16 |  |  |  | (0.09) |  |  | 
 | Tyre 3 |  |  |  | Tyre 4 |  |  | 
Groove | B | C | D | E | B | C | D | E
Average tread-depth before buffing | 6.87 | 6.98 | 6.96 | 6.76 | 6.90 | 7.01 | 6.98 | 6.75
Buffing target(2.45mm offset) | 4.42 | 4.53 | 4.51 | 4.31 | 4.45 | 4.56 | 4.53 | 4.30
Average Buffing target | 4.44 |  |  |  | 4.46 |  |  | 
Average Individual tread-depth after buffing | 4.58 | 4.69 | 4.64 | 4.30 | 4.61 | 4.70 | 4.64 | 4.40
Average tread-depth after buffing | 4.55 |  |  |  | 4.58 |  |  | 
Deviation of Average Individual tread-depth | 0.17 | 0.17 | 0.12 | (0.01) | 0.17 | 0.14 | 0.10 | 0.10
Deviation of Average tread-depth total measurements | 0.11 |  |  |  | 0.13 |  |  | 
Example 1
Model : 245/40 R18
Scenario : 2.45mm offset buffing
Remark : This is a conventional grinding scenario that the tolerance is allowed to accumulate on both sides.

## Slide 10: Buffing Tolerance of Example 1
10
245/40 R18
(2.45mm offset buffing )
Chart: Measurement position
tolerance 0.4 | 0.4 | 0.4 | 0.4 | 0.4
tolerance -0.4 | -0.4 | -0.4 | -0.4 | -0.4
Devi of ave indiv tread-depth for Tire 1 | 0.22 | 0.18 | 0.13 | 0.09
Devi of ave indiv tread-depth for Tire 2 | -0.03 | -0.07 | -0.11 | -0.12
Devi of ave indiv tread-depth for Tire 3 | 0.17 | 0.17 | 0.12 | -0.01
Devi of ave indiv tread-depth for Tire 4 | 0.17 | 0.14 | 0.1 | 0.1
Upper limit
Lower limit

## Slide 11: Example 2
11
 | Tyre 1 |  |  |  | Tyre 2 |  |  | 
Groove | B | C | D | E | B | C | D | E
Average tread-depth before buffing | 7.19 | 7.46 | 7.36 | 6.95 | 6.92 | 7.34 | 7.33 | 6.85
Buffing target | 3.60 | 3.73 | 3.68 | 3.48 | 3.46 | 3.67 | 3.66 | 3.42
Average Buffing target | 3.62 |  |  |  | 3.55 |  |  | 
Average Individual tread-depth after buffing | 3.90 | 3.86 | 3.76 | 3.74 | 3.62 | 3.62 | 3.45 | 3.39
Average tread-depth after buffing | 3.82 |  |  |  | 3.52 |  |  | 
Deviation of Average Individual tread-depth | 0.30 | 0.13 | 0.08 | 0.27 | 0.16 | (0.06) | (0.22) | (0.04)
Deviation of Average tread-depth total measurements | 0.20 |  |  |  | (0.03) |  |  | 
 | Tyre 3 |  |  |  | Tyre 4 |  |  | 
Groove | B | C | D | E | B | C | D | E
Average tread-depth before buffing | 6.34 | 6.86 | 6.76 | 6.26 | 6.84 | 7.28 | 7.28 | 6.76
Buffing target | 3.17 | 3.43 | 3.38 | 3.13 | 3.42 | 3.64 | 3.64 | 3.38
Average Buffing target | 3.28 |  |  |  | 3.52 |  |  | 
Average Individual tread-depth after buffing | 3.62 | 3.52 | 3.40 | 3.49 | 3.87 | 3.87 | 3.66 | 3.60
Average tread-depth after buffing | 3.51 |  |  |  | 3.75 |  |  | 
Deviation of Average Individual tread-depth | 0.45 | 0.09 | 0.02 | 0.36 | 0.45 | 0.24 | 0.03 | 0.22
Deviation of Average tread-depth total measurements | 0.23 |  |  |  | 0.23 |  |  | 
Model : 225/45 R19
Scenario : 50% offset buffing
Remark : The tolerance is only allowed to accumulate on one side.

## Slide 12
12
Chart: Mesurement position
tolerance 0.4 | 0.4 | 0.4 | 0.4 | 0.4
tolerance -0.4 | -0.4 | -0.4 | -0.4 | -0.4
Devi of ave indiv tread-depth for Tire 1 | 0.3 | 0.13 | 0.08 | 0.27
Devi of ave indiv tread-depth for Tire 2 | 0.16 | -0.06 | -0.22 | -0.04
Devi of ave indiv tread-depth for Tire 3 | 0.45 | 0.09 | 0.02 | 0.36
Devi of ave indiv tread-depth for Tire 4 | 0.45 | 0.24 | 0.03 | 0.22
Upper limit
Lower limit
225/45 R19
(50% offset buffing )
Buffing Tolerance of Example 2

## Slide 13: Buffing Tolerance Comments
13
Individual tread-depth: 2,0 +/- 0,4mm
Average tread-depth in principal groove: 2,0 +/- 0,3mm
Average tread-depth total measurements: 2,0 +/- 0,2 mm
Following the document WT-02-02 , ETRTO considers buffing tolerance limits as follows：
Comments:
According to the current tests’ results, we consider that the buffing tolerance is acceptable through a current buffing machine.
BUT it shows also a negative result when choosing a different buffing scenario (e.g. 50% offset buffing).
More work is in progress right now…

## Slide 14
14
III. Additional Information

## Slide 15: Additional information on Tyre buffing
15
Grinding wheel rotation direction:
Easier to buff the tyre if opposite to the tyre rotation.
Additional assessments are needed to measure any influence on buffing roughness.
Buffing temperature：
Stop buffing when tread temperature reach to 45℃, tread compound needs to be cooled down to avoid possible damages.
Number of grinding cycles：
Affect buffing uniformity and grinding amount.
Additional assessments are needed to find the particulars.

## Slide 16: IV. Conclusions
16
The requirement about buffing tolerance is acceptable according to the current practices.
Both buffing scenarios can be achieved, additional assessments are needed to determine which scenario is better.
Several factors are found to influence the buffing effect, such as grinding wheel rotation direction, number of grinding cycles, buffing temperature and so on.

## Slide 17
Web site：www.catarc.org.cn
17
Thanks for your attention
National Automotive Standardization Technical Committee